308,309,232 A & B,G.I.D.C. Estate,At Dediyasan,Mehsana - 384002 Gujarat India

Contact Number :  , Email : info@gujprintpack.com

GSTIN :  24AAACG7781P1Z1, IEC CODE : 0894007882, PAN : AAACG7781P

Gujarat Print Pack Publications Pvt. Ltd.

Certificate of Analysis [COA] For Label

Production Order No.

COA Date :  04/01/2022

Delivery No.

33858

Client Name

Weener Empire Plastic P Ltd.[Masat]

GP3 Code

Client Item Code 1

Client Item Code 2

FGLA8400

PMLB0070

1463000707006001

Product Name

Dr. fixit 301 URP pidicrete 1kg F & B Label Rev3

Specified Size

Width(mm)

Length(mm)

Client's Specified Size

70

115

Tested Size

70

115

LABEL STOCK

Face Material

Adhesive

Release Liner

Material

Required

27 GSM

80 GSM /Microns

60 GSM

Tested

80 GSM/Microns

26 GSM

59 GSM

Type Required

Glassine

HotMelt

Chromo

Observed

Glassine Paper

Rubber Based (Hot Melt)

Chromo

PRINTING

No. of Colors

1

2

3

4

5

6

7

8

9

10

Given By Client

Magenta

Cyan

Yellow

Black

Blue

P.151C

Color Shade Verified

OK

OK

OK

OK

OK

OK

Shade Match Grade

4

Remarks For Shade :

Shade found to be a satisfactory match against sample

Text  Matter Verification With Specified Art Work

Remarks For Text Verification

Pass

Text matter verified to be matching with control samples

Bar Code Grade

Bar Code Remarks

COATING

Aqueous

U.V

Lamination

Minimum Gloss Required at 60

35%

72%

75%

Scuff Test

84.00%

Coating Done :

Gloss UV

Achieved Gloss

2 lbs, 100 rounds Okay

Die Cutting Type

Finishing Quality Grade

4

Rectangle with radius corner

FINISHING

Die Cutting

Rewinding Quality

Okay

Okay

Emboss

Packing Quality

Okay

Not Applicable

Foil Stamping

Slitting Quality

Okay

Not Applicable

Remarks For Finishing Quality

Finishing Quality Found to Be Satisfactory

Final Inspection

Passed

Over All Quality Remarks

Overall quality found to be satisfactory

TOLERANCE

Field

Length

Width

Face Material

Adhesive

Release Liner

+

2 mm

2 mm

10 %

2 GSM

5 %

-

2 mm

2 mm

10 %

2 GSM

5 %

All Grades are given on a scale of 5

Where testing is not possible result may be reported based on supplier's COA

This material should be retested on 03/07/2022 before usage.

THIS IS A SYSTEM GENERATED DOCUMENT.  IT DOES NOT REQUIRE A SIGNATURE.