308,309,232 A & B,G.I.D.C. Estate,At Dediyasan,Mehsana - 384002 Gujarat India

Contact Number :  , Email : info@gujprintpack.com

GSTIN :  24AAACG7781P1Z1, IEC CODE : 0894007882, PAN : AAACG7781P

Gujarat Print Pack Publications Pvt. Ltd.

Certificate of Analysis [COA] For Shrink Sleeves

Production Order No.

COA Date :

Delivery No.

33814

Client Name

The Unjha Pharmacy

GP3 Code

Client Item Code 1

Client Item Code 2

FGSL0395

Product Name

Narogi Churana 100g Sleeve Rev-1

Specified Size

Open Width(mm)

Cut Length(mm)

Client's Specified Size

152.40

168.00

Tested Size

152

168

SLEEVE FILM

Thickness(Microns)

Shrinkage Ratio (%)

Type

Material

Required

Centroiid Plastopack PVC Blown 40 mic 200 mm

50

40

Tested

40

PVC Blown

49

PRINTING

No. of Colors

1

2

3

4

5

6

7

8

9

10

Given By Client

Magenta

Cyan

Yellow

Black

Gold White

Color Shade Verified

OK

OK

OK

OK

OK

Shade Match Grade

4

Remarks For Shade :

Shade found to be a satisfactory match against sample

Text  Matter Verification

Remarks For Text Verification

4

Text matter verified to be matching with control samples

Bar Code Grade

Bar Code Remarks

4

Bar Code Scanned and Quality Found to be Satisfactory

COATING

Aqueous

U.V

Lamination

Minimum Gloss Required at 60

35%

72%

75%

Coating Done :

Matt UV

Achieved Gloss

Scuff Test

2 lbs, 100 rounds Okay

50%

Finishing Quality Grade

4

FINISHING

Perforation Quality

Rewinding Quality

Not Applicable

Not Applicable

Holding Glue Quality

Packing Quality

Okay

Okay

White Opacity

Slitting Quality

Okay

Not Applicable

Remarks For Finishing Quality

Finishing Quality Found to Be Satisfactory

Final Inspection

Passed

Over All Quality Remarks

Overall quality found to be satisfactory

TOLERANCE

Field

Cut Length

Open Width

Shrinkage Ration

Microns

+

2 mm

2 mm

5 %

10 %

-

2 mm

2 mm

5 %

10 %

All Grades are given on a scale of 5

Where testing is not possible result may be reported based on supplier's COA

Shrink Sleeves are heat sensitive.Material is valid only if stored under 30 degrees Celsius.

This material should be retested on  before usage.

THIS IS A SYSTEM GENERATED DOCUMENT.  IT DOES NOT REQUIRE A SIGNATURE.