| Supplier Name |  | Report number |  |
| --- | --- | --- | --- |
| Product Description |  | SAP Batch number |  |
| GRN Qty. |  | GRN number |  |
|  |  | Date of Inspection |  |

| SR. NO. | TEST PARAMETERS | SPECIFICATION | OBSERVATION |
| --- | --- | --- | --- |
|  | Code No. | As per PO |  |
|  | SHADE | Should match to the master or the specimen Or To Pantone Code No |  |
|  | SPECTROMETER SHADE RANGE (dE) | Delta Value DE should be below 3.0 |  |
|  | Skinning | Very thick top layer skinning & solid particles not acceptable |  |
|  | Flow rate | Max. 120 mm (Except Silver & Gold ink) |  |
|  | Drying test | By Thumb Impression : No Inking of the thumb after rubbing the roll up of one big & one small drop of ink dried for 24 hrs. |  |
|  |  | On Glass surface : For Solid Print Immediately drying (with in 1 hrs) For small drops of ink dried for 24hrs |  |
|  | Alkali resistance (AR Test) | If Specified in P.O. then No fading of ink roll up in 2% NaOH Solution for 24hrs |  |
|  | Soap resistance (SR Test) | If Specified in P.O. then No staining of ink roll up to 20 % soap jelly kept for 24hrs |  |
|  | Light fastness test | No fading of the ink roll up when exposed to direct sun for 80hrs. |  |

| LOT STATUS | ACCEPTED | REJECT & SEND BACK TO SUPPLIER / SCRAP | SEGREGATION | ACCEPTED ON DEVIATION |
| --- | --- | --- | --- | --- |
| REASON FOR DEVIATION / REJECTION / SEGREGATION |  |  |  |  |

| INSPECTED BY | APPROVED BY |
| --- | --- |
| QA INSPECTOR | QA MANAGER |